# Grain Size Analysis Report

Project; Project. Report Date; June 30, 2026 at 14:44.

Sample Name; Example_1_Case_1_Vukovic. Soil Classification; Poorly-graded sand. Temperature; 20.0°C. Porosity; 0.3838. Porosity Source; Calculated (Simple formula). Data Points; 7.

## Executive Summary

Sample Example_1_Case_1_Vukovic has been analyzed and classified as Poorly-graded sand .

| Median Size (D₅₀) 0.485 mm | Uniformity (Cu) 3.67 Uniform | Curvature (Cc) 1.48 Well-graded (1 ≤ Cc ≤ 3) |
| --- | --- | --- |

## Methodology

### Grain Size Distribution Analysis Grain size distribution was determined using sieve analysis and/or sedimentation methods following standard geotechnical procedures. The cumulative distribution curve plots percent passing versus grain size on a semi-logarithmic scale.

### Characteristic Diameters Characteristic grain sizes represent specific percentiles of the grain size distribution: D₁₀, D₃₀, D₅₀, D₆₀: Grain diameters at which 10%, 30%, 50%, and 60% of the soil mass is finer D₅₀ (Median): The median grain size, representing the center of the distribution These values are fundamental for soil classification and hydraulic conductivity estimation

### Gradation Parameters Uniformity Coefficient: Cu = D₆₀ / D₁₀ Cu < 4: Uniform gradation (narrow size range) 4 ≤ Cu < 6: Moderate gradation Cu ≥ 6: Well-graded soil (wide size range) Coefficient of Curvature: Cc = (D₃₀)² / (D₁₀ × D₆₀) 1 ≤ Cc ≤ 3: Well-graded with good particle size distribution Outside this range: Gap-graded or uniform distribution

## Results & Analysis

### Characteristic Grain Sizes

| D₁₀ 0.150 mm | D₃₀ 0.350 mm | D₅₀ 0.485 mm | D₆₀ 0.550 mm |
| --- | --- | --- | --- |

### Soil Classification Parameters

| Parameter | Value | Classification |
| --- | --- | --- |
| Uniformity Coefficient (Cu = D₆₀/D₁₀) | 3.67 | Uniform |
| Coefficient of Curvature (Cc = D₃₀²/D₁₀·D₆₀) | 1.48 | Well-graded (1 ≤ Cc ≤ 3) |
| Soil Classification | Poorly-graded sand |  |

### Gradation Analysis

Label (ISO 14688 / DS/EN ISO 14688): Poorly-graded sand

Descriptor: Moderately well sorted sand low in fines

| Sub-class | Size range (mm) | Percentage |
| --- | --- | --- |
| Clay | < 0.002 | 0.0% |
| Fine silt | 0.002 – 0.0063 | 0.0% |
| Medium silt | 0.0063 – 0.02 | 0.0% |
| Coarse silt | 0.02 – 0.063 | 2.8% |
| Fine sand | 0.063 – 0.2 | 11.8% |
| Medium sand | 0.2 – 0.63 | 52.2% |
| Coarse sand | 0.63 – 2 | 33.2% |
| Fine gravel | 2 – 6.3 | 0.0% |
| Medium gravel | 6.3 – 20 | 0.0% |
| Coarse gravel | 20 – 63 | 0.0% |
| Cobble | 63 – 200 | 0.0% |

#### Calculation Internals

| Physical constants | Value |
| --- | --- |
| g (gravity) | 980 cm/s² |
| ρ water density | 0.9981 g/cm³ |
| μ water viscosity | 0.00985 g/(cm·s) |
| ρg/μ | 9.933e+04 /(cm·s) |
| τ (Sauerbrei) | 1.053 |
| Temp. correction | 1.000 (20 °C ref) |

| Effective diameters dₑ | Value |
| --- | --- |
| Kruger | 0.0344 cm · 0.344 mm |
| Kozeny-Carman (harmonic) | 0.0290 cm · 0.290 mm |
| Zunker | 0.0307 cm · 0.307 mm |
| Zamarin | 0.0326 cm · 0.326 mm |
| Geometric mean d_geom | 0.4497 mm |
| Alyamani-Sen Iₒ → dₑ | 0.0663 → 0.0746 mm |

| Sorting (φ units · Krumbein-Monk input) | Value |
| --- | --- |
| D5 φ = log₂(d) | -3.36 |
| D16 φ = log₂(d) | -2.13 |
| D50 φ = log₂(d) | -1.04 |
| D84 φ = log₂(d) | 0.08 |
| D95 φ = log₂(d) | 0.77 |
| σφ (sorting) | 1.18 |

| Porosity functions fₙ | Value |
| --- | --- |
| void ratio e = n/(1−n) | 0.623 |
| n/(1−n)² (Kruger) | 1.011 |
| n³/(1−n)² (Sauerbrei·K-C·Zamarin·Barr) | 0.149 |
| (n/(1−n))² (Zunker) | 0.388 |
| Zamarin Cₙ = (1.275−1.5n)² | 0.489 |

## Grain Size Distribution Curve

Figure 1: Cumulative grain size distribution curve for Example_1_Case_1_Vukovic

## Grain-size Class Histogram

Figure 2: Retained weight by classification class for Example_1_Case_1_Vukovic

## Hydraulic Conductivity by Method

Figure 3: Estimated hydraulic conductivity by method for Example_1_Case_1_Vukovic

# Appendices

### Appendix A: Detailed Percentile Data Percentile; Size (mm); Relative (%). D5; 0.098; 5%. D10*; 0.150; 8%. D16; 0.228; 13%. D20; 0.280; 16%. D25; 0.315; 18%. D30*; 0.350; 20%. D40; 0.420; 24%. D50*; 0.485; 28%. D60*; 0.550; 32%. D75; 0.752; 44%. D84; 1.056; 61%. D90; 1.410; 82%. D95; 1.705; 100%.